## Slide 1
Felix Hartz
Master Talk
9/19/2017
Electrical Readout of NVˉ Centers in Diamond
Notes: Grundstruktur:
Einführung: NV- ist toll
NV Zentrum Levelschema
ESR, optisch detektiert (ODMR), erkläre im Levelschema, dann zeige ODMR Setup. Am Ende der Folie sage ich, dass ODMR aufwändig ist (Filter, APD, Lange Wartezeiten (bei kleiner Countrate, Effizienz, …)
Deshalb: elektrisch von Vorteil: pEDMR (viel zeit lassen, ausführlich Dynamik diskutieren
(leider kleiner Strom, muss verstärkt werden, was das ganze Detektionsverfahren langsam macht)
Darauf basierend erkläre ich meine Stromauslese endlich, indem ich das zweite Setupbild zeige.
Danach MSM Detektor

## Slide 2: Outline
Motivation
Theory
NVˉ Spectrometer
Summary and Outlook
Spin-to-Charge Conversion
Felix Hartz
9/19/2017
2
Notes: Theory of Physical principles we use for readout of NV
Introduce new spectrometer, show spin resonance experiments
Discuss the level diagram of nv- and how this knowledge can be used for improvement of spin to charge conversion
BEFORE I come to the conclusions and an outlook

## Slide 3
single NV- center magnetometer
Motivation
Maletinsky et al., Nature Nanotechnology 7 (2012)
N. Bar-Gill, Nature Communications 4,1743 (2013)
time (ms)
long spin coherence time
signal (normalized)
Felix Hartz
9/19/2017
3
Notes: Diamond nanopillar with single NV: scan hard disk magnetic field domains
Spin coherence can be enhanced by applying a pulse sequence multiple times

## Slide 4
NVˉ Center in Diamond
D
E
Christle, Nature Materials 14, 160 (2015)
microwave photons
Ephoton=ħf
B0
+1
0
-1
ms
Hamiltonian for spin system
C
N
V
Felix Hartz
9/19/2017
4
H=mbgSB0 + SDS
^
Gali et al., Phys. Status Solidi B 248, 1337 (2011)

## Slide 5
Coherent Spin Control
nutation of spin vector S
wnut  amplitude of BMW
D  frequency of BMW
BMW
S
Felix Hartz
9/19/2017
5
rotating frame system
S
BMW
M. H. Levitt: Spin Dynamics (Wiley, 2001)
Christle, Nature Materials 14, 160 (2015)
Hamiltonian
nutaion frequency
ħwnut =gmbBMW
H=mbgSBMW + SDS
^
spin vector

## Slide 6
Robledo, NJP 13, 025013 (2011)
Felix Hartz
9/19/2017
NVˉ Level Diagram
dark state
Notes: Opt ground state triplet
Opt excited, spin conserving optical transitions
(CYCLING) for ms = 0
Schelfing into dark state for ms 1
For ms=0: ionization out of excited NV-

## Slide 7
Optical Readout
Felix Hartz
9/19/2017
7
Ub
U
Electrical Readout

## Slide 8
High Purity Diamond Sample
bias voltage
Ub
200 mm
microscope image
type IIa diamond, [N] < 1 ppm
interdigital contacts, 10 mm gap
oxygenated surface with
Ti/Au metallization: Schottky barrier
back-to-back diode
Felix Hartz
9/19/2017
8

## Slide 9
Photocurrent Detection: Depth Dependence
Felix Hartz
9/19/2017
9
y
x
z
high resolution
100x objective
homogeneous illumination
5x objective

## Slide 10
Felix Hartz
9/19/2017
10
Photocurrent Detection: Lateral Dependence
y
x
z
photocurrent (pA)
metal contacts
photocurrent (pA)

## Slide 11
Electrical versus Optical Readout
readout method | optical | electrical
res. frequency (MHz) | 2870.04 ± 0.04 | 2870.14 ± 0.07
linewidth (MHz) | 14.90 ± 0.15 | 13.3 ± 0.13
spin-contrast (%) | -(14.4 ± 0.2) | -(12.6 ± 0.2)
room temperature
frequency f
Felix Hartz
9/19/2017
11
bias voltage
Ub
Notes: 1 Pulse sequence: mw pulse initializes NV spin, green laser excitation and ionization of NV-
When spin prepared to ms1, shelfing into dark state
2 table: the same resonance frequency within the small error bars (40-70 kHz)
(df/f=70 000 für pEDMR, 40000 for ODMR)
linewidth smaller in pEDMR: different excitation volume, linewidth narrowed under higher excitation power
Contrast comparable, function of the laser intensity and duration

## Slide 12
Coherent Control
microwave
pulse duration
Felix Hartz
9/19/2017
12
MW wire
BMW (mT)
wnut (mT)
bias voltage
Ub
Notes: 1 Flat off res data, in resonance spin transitions induced, depending on tMW.
2 tmin varies with distance.
When t is used to derive B that is assumed to decrease with 1/R
assuming R1=180 and R2 / 240 (R0=180, Feld dort 0.15 mT), tpi=120 ns

## Slide 13
Spin-to-Charge Conversion (SCC)
Measurement and Control of Single Nitrogen-Vacancy Center Spins above 600 K
D. M. Toyli, D. J. Christle, A. Alkauskas, B. B. Buckley, C. G. Van de Walle, and D. D. Awschalom
Phys. Rev. X 2, 031001 – Published 5 July 2012
Dark state excited state \5> : ~0.8 eV unter \3>,\4>
Felix Hartz
9/19/2017
13
Nesladek, APL, 72, 3306, (1998)
Schields, PRL 114, 136402 (2015)
Hopper, PRB 94, 241201(R) (2016)
Chen, PRB 92, 104301 (2015)
Chen, PR Appl. 7, 014008 (2017)
Bourgeois, PRB 95, 041402(R) (2017)
Notes: To scale, bandgap -5.45 eV, arrows to scale
NV- shaded area: uncertainty of the energy level
NV0
Ns0 substitutional, neutral charge state, can be ionized

## Slide 14
Linear Photoionization of NVˉ
+5 V
Felix Hartz
9/19/2017
14

## Slide 15
NIR Laser
green laser
power
Felix Hartz
9/19/2017
15

## Slide 16
Spin-independent Charge-Conversion Efficiency
N. Aslam, New Journal of Physics 15, 013064 (2013)
Felix Hartz
9/19/2017
16
non-destructuve detection of the charge state
NVˉ
NV0
NV0
dominant charge state

## Slide 17
Spin-to-Charge Conversion: Schields
Felix Hartz
9/19/2017
17
NVˉ
NV0
NVˉ
NV0
Schields, PRL 114, 136402 (2015)
ms = 0
ms = 1
ms = 0
ms = 1
ms = 0
ms = 1
tshelf (ns)
SCC contrast (%)
SCC contrast (%)
tion (ns)
tshelf = 60 ns
tion = 20 ns

## Slide 18
Summary
first studies on dual-laser excitation SCC
verification and concretisation of NVˉ level diagram
demonstration of SCC at the new NVˉ spectrometer (electrical and optical)
Felix Hartz
9/19/2017
18

## Slide 19
Outlook: Multi-Laser Pulse Sequences for SCC
SCC method | optical | electrical
contra | long readout time after each SCC step | photocurrent contribution from Ns0, slow (transimpedance amplifier / lock-in)
pro | high SCC contrast | no detection optic required, possibly faster (single electron transitor)
feedback: 1 dimensional
photocurrent / photoluminescence
optimized pulse sequences
reflection
2 dimensional
Felix Hartz
9/19/2017
19

## Slide 20
Thank you for your attention.
Special thanks to:
Prof. Martin Brandt
Prof. Martin Stutzmann
Florian Hrubesch
E25 group
Felix Hartz
9/19/2017
20

## Slide 21
Spin-to-Charge Conversion (SCC)
Measurement and Control of Single Nitrogen-Vacancy Center Spins above 600 K
D. M. Toyli, D. J. Christle, A. Alkauskas, B. B. Buckley, C. G. Van de Walle, and D. D. Awschalom
Phys. Rev. X 2, 031001 – Published 5 July 2012
Dark state excited state \5> : ~0.8 eV unter \3>,\4>
Felix Hartz
9/19/2017
21

## Slide 22
Felix Hartz
SCC: Charge State Initialization
linit (nm) | NVˉ propability | data | reference
532 | 75 %, 74.2 % |  | Hrubesch 2017, Chen 2015, PHYSICAL REVIEW B 92, 104301 (2015)
637 | 6% |  | Chen 2015, PHYSICAL REVIEW B 92, 104301 (2015)
405 | 48.8 % |  | Chen 2015, PHYSICAL REVIEW B 92, 104301 (2015)
532 | 72.3 % (97.5 % optimized) |  | Schields, PRL 114, 136402 (2015)
450-610 | 0<p<75% as a function of linit |  | N. Aslam, New Journal of Physics 15, 013064 (2013)
~900-1000 (spectrum) | 70- 90 % as a function of PNIR |  | Hopper, PHYSICAL REVIEW B 94, 241201(R) (2016)
Felix Hartz
9/19/2017
22

## Slide 23
electical readout | linit (nm) | lshelf (nm) | lion (nm) | initial spin polarization | SCC contrast | reference
single laser | 532 520 | 532 520 | 532 (2) 520 (2) | 75 % (fitted value) - | -14 % -13.5 % | Hrubesch Hartz
dual laser | 532 | 532 | 450 (1) |  | -9 % | Bourgeois
optical readout |  |  |  |  |  | 
triple laser | 532 | 594 | 638 (2) |  | -70 % | Schlieds
dual /triple | 532 | 637 | 405 |  | -10 % | Chen 2015
triple laser | 532 | 637 | 780 |  | -5 % | Chen 2017
NIR laser assisted | 532 | 532 | 900-1000 spectrum | 85% | -7 % | Hopper
Overview: SCC Methods
overview Laser energieswork edition |  | NV- ZPL (nm) | NV0 ZPL (nm) |  | Reference
 |  | 637 | 575, 2.156 eV |  | N. Aslam, New Journal of Physics 15, 013064 (2013)
 |  | 1042 nm, 1.19 eV | 785 nm 1.58 eV | 780 nm, 1.59 eV | 
 |  | 2.38 eV, 520 nm | 2.33 eV, 532 nm |  | 
 | 405 nm, 3.06134 eV |  |  |  | Chen 2015
 | 900-100, 1.38-1.24 |  |  |  | 
Felix Hartz
9/19/2017
23
method | linit (nm) | lshelf (nm) | lion (nm) | initial spin polarization | SCC contrast | reference
Single green laser | 532 520 | 532 520 | 532 (2) 520 (2) | 75 % (fitted value) - | -14 % -13.5 % | Hrubesch Hartz
Dual laser excitation | 532 | 532 | 450 (1) |  | -9 % | Gulka, Nesladek
Triple laser excitation | 532 | 594 | 638 (2) |  | -80 % (nachrechnen) | Schlieds
 | 532 | Recombination and ionization rates 560 vs 590 nm (quadratic both) |  |  |  | Aslam 2013
 |  |  | 405 (1) |  |  | Chen 2015
 | 532 | 637 | 780 |  | -5 % | Chen 2017
Dual (laser) exciation Or: NIR laser assisted | 532 | 532 | 900-1000 spectrum | 85% | -7 % | Hopper 2016
method | linit (nm) | lshelf (nm) | lion (nm) | initial spin polarization | SCC contrast | reference
Single green laser | 532 520 | 532 520 | 532 (2) 520 (2) | 75 % (fitted value) - | -14 % -13.5 % | Hrubesch Hartz
Dual laser excitation | 532 | 532 | 450 (1) |  | -9 % | Gulka, Nesladek
Triple laser excitation | 532 | 594 | 638 (2) |  | -70 % | Schlieds
 | 450-620 | Recombination and ionization rates 560 vs 590 nm (quadratic both) |  |  |  | Aslam 2013
 | 532 | 637 | 405 |  | -10 % | Chen 2015
 | 532 | 637 | 780 |  | -5 % | Chen 2017
Dual (laser) exciation Or: NIR laser assisted | 532 | 532 | 900-1000 spectrum | 85% | -7 % | Hopper 2016
Schields, PRL 114, 136402 (2015)
Hopper, PRB 94, 241201(R) (2016)
Chen, PRB 92, 104301 (2015)
Hrubesch, PRL 118, 037601 (2017)
method | linit (nm) | lshelf (nm) | lion (nm) | initial spin polarization | SCC contrast | reference
single laser | 532 520 | 532 520 | 532 (2) 520 (2) | 75 % (fitted value) - | -14 % -13.5 % | Hrubesch Hartz
dual laser | 532 | 532 | 450 (1) |  | -9 % | Gulka, Nesladek
triple laser | 532 | 594 | 638 (2) |  | -70 % | Schlieds
dual /triple | 532 | 637 | 405 |  | -10 % | Chen 2015
triple laser | 532 | 637 | 780 |  | -5 % | Chen 2017
NIR laser assisted | 532 | 532 | 900-1000 spectrum | 85% | -7 % | Hopper 2016
Chen, PR Appl. 7, 014008 (2017)
Bourgeois, PRB 95, 041402(R) (2017)
Notes: Hrubesch compared to Hartz: less laser power required for SCC (4-5x less, pulse durations are the same)

## Slide 24
Overview level Diagrams and SCC Methods
Felix Hartz
9/19/2017
24
Bourgeois
Hopper
Schields
Hrubesch / Hartz
Chen

## Slide 25
SCC Hopper
Felix Hartz
9/19/2017
25
Hopper, PHYSICAL REVIEW B 94, 241201(R) (2016)

## Slide 26
Possible Readout Techniques
Dual-laser Nesladek, Bourgeois
Felix Hartz
9/19/2017
26

## Slide 27: Aslam ionization, recharging

## Slide 28: NIR noise

## Slide 29
Photoconductive Gain
photoconductive gain factor
where
Felix Hartz
9/19/2017
29

## Slide 30
Metal Semiconductor Metal Photodetector
+5 V
Felix Hartz
9/19/2017
30

## Slide 31
Dual Laser Spin-to-Charge Conversion
Felix Hartz
9/19/2017
31

## Slide 32
Dual Laser Spin-to-Charge Conversion
Felix Hartz
9/19/2017
32

## Slide 33
Current-Voltage Characteristic
bias voltage
Ub
Felix Hartz
9/19/2017
33

## Slide 34
Coherent Control
microwave
pulse duration
Felix Hartz
9/19/2017
34
MW wire
BMW (mT)
wnut (mT)
Notes: 1 Flat off res data, in resonance spin transitions induced, depending on tMW.
2 tminimum varies with distance of mw wire. When t is used to derive B that goes with 1/R assuming R1=180 and R2 / 240 (=R0=

## Slide 35
NIR Laser
green laser
power
Felix Hartz
9/19/2017
35
Notes: Level Diagramm mit allen 5 NV states, to scale!!!
N_s^0 States, Rohrer Spectrum!!!, abs setzt ein bei bereits 1 eV
Zeige pedmr experimente von Chen,
Optisches auslesen von NV spin mit green, NIR pulse sequence

## Slide 36
Spin-independent Charge-Conversion Efficiency
NVˉ
NV0
NV0
dominant charge state
N. Aslam, New Journal of Physics 15, 013064 (2013)
Felix Hartz
9/19/2017
36

## Slide 37
non-destructuve detection of the charge state
N. Aslam, New Journal of Physics 15, 013064 (2013)
Spin-independent Charge-Conversion Efficiency
Felix Hartz
9/19/2017
37